CLEANING & MAINTAINING YOUR

WATERBORNE POLYURETHANED TIMBER FLOOR

Polyurethaned floors are sanded, trowel filled & coated with 3 coats of water based polyurethane of either a matt or satin finish.   In general, reapplication of polyurethane coatings is necessary only when damage occurs,  or after 7-10 years of typical wear. Polyurethane is not waterproof, only water-resistant and excess water will seep through the coatings causing damage. These floors are not waxed, polished or buffed to maintain them – just cleaned.

IN GENERAL

Preferably use dry (spray on & wipe off), not wet (mop & bucket), cleaning methods.

Keep dirt and grit off the floor as it can be ground in and damage coatings

Use protective mats inside and outside exterior doorways

Wipe up spills ASAP with a slightly damp cloth and remove excess moisture with a dry mop or cloth immediately

Use mats and/or floor felts under heavy furniture and movable objects (chairs, etc.) to prevent markings

Don’t use excessive water or let water sit on timber flooring. On completion of cleaning/mopping, the floor should be dry.

Check your vacuum cleaner wheels and head won’t leave scratches, use a brush rather than hard head.

Don’t use steam mops, soaps, detergents, kerosene or “oil soaps”.  They may damage the wood and the finish and may leave a discolouring residue. The specialised cleaner specifically recommended for your floor coating is ideal.

Don’t drag anything across the timber flooring, this can result in scratches, gouges & dents in the floor.

EQUIPMENT, MATERIALS AND PERIODICITY

Vacuums and dry mops are both dry cleaning methods. Dry mops are not dipped in a bucket of water – cleaner is sprayed on the floor or on to the mop head. We recommend a mop with a flat head and removable light cover/s. These mops are available from Just Hardwood Floors.

The suggested frequency for cleaning a timber floor is simple … as often as you would like. Vacuum or sweep the floor regularly to remove loose dirt, dust and gritty particles prior to mopping. OR, for light cleaning use a dry mop with an anti-static cover for picking up dust. . If you are using the correct cleaning method and solution, even daily cleaning will not damage your floor.  Most cleaning solutions can be diluted for general, heavy and spot cleaning.   The regularity of floor cleaning is often tied to the traffic level over the floor and the frequency of vacuuming.

POLYURETHANED TIMBER FLOORING

Bona Wood Floor Cleaner is the recommended product for cleaning your polyurethaned floors.

Bona floor cleaner can be sprayed on in a fine mist and wiped off with a dry or damp cloth.

Further bottles of Bona floor cleaner are available from Just Hardwood Floors for $20.00 per 1L bottle.

# Text boxes

Feltac Felt Pads

We highly recommend Feltac self-adhesive pads to prevent your furniture damaging your timber floor. Feltac pads are a heavy duty, dense, self-adhesive felt pad. Just peel off the backing and stick them to the bottom of your furniture. They come in a wide range of sizes that will suit anything you have in your home.

Felt pads should be placed on movable items (eg chairs) to prevent scratches and on non-movable items (eg tables and cabinets) to prevent dents. The felts will not compress with age and the self adhesive layer bonds firmly so they offer quality, durable protection.

Protects floors and walls		Adds feeling of softness

Superior quality			Makes furniture easier to move

Ultra-strength adhesive		Highly durable

19mm Round Discs Beige (20 Pieces)		17048		$7.50 incl.

25mm Round Discs Beige (16 Pieces) 		17042		$7.50 incl.

38mm  Round Discs Beige (6 Pieces) 		17043		$8.50incl.

114x152mm Two Piece Rectangle Beige		17041		$12.50 incl.

Various Multipack Beige (33 Pieces)		23054		$13.50 incl.

Floor Cleaning Products

Bona Wood Floor Cleaner is the recommended product for cleaning your waterborne polyurethaned floor.

Unlike most other cleaning solutions, it will not leave a build-up or residue on the floor and it contains a drying

agent to prevent water marks being left after cleaning.

1 Litre Spray Bottle				$20.00 incl.

Sabco Mop with Wet and Dry Covers	$40.00 incl.

Sabco Replacement Wet Covers		$15.00 incl.

Bona Spray Mop				$85.00 incl

Bona Replacement Covers			$20.00 incl

Maintenance Products  (prices as at January 2018)

The following products, available from our showroom, are recommended for use with solid timber, timber veneer  and laminate flooring.  Visit us or phone through your order and we can courier your order (delivery charge applies).